## Slide 1
SCIANTIX: Advanced developments
Hands on the source code
Developer side: Editing and (re)compiling
Advanced modelling: Machine Learning with SCIANTIX
Survey
Giovanni Zullo
Lyon, France, 15.05.2024

## Slide 2
SCIANTIX: Advanced developments
Hands on the source code
Developer side: Editing and (re)compiling
Advanced modelling: Machine Learning with SCIANTIX
Survey
Giovanni Zullo
Lyon, France, 15.05.2024

## Slide 3: Hands on the source code
Temporal loop
Input reading & initialization
Closing execution
MainSCIANTIX.C
Sciantix.C/h

## Slide 4: Hands on the source code
Temporal loop
Input reading & initialization
Closing execution
Solvers
Simulation
Models
MainSCIANTIX.C
Sciantix.C/h
_options
_history
_variables
_scaling_factors
_diffusion_modes
objects

## Slide 5: Hands on the source code
Sciantix.C/h
Set
Update
Simulation

## Slide 6: Hands on the source code
Sciantix.C/h
Set
Update
Simulation
SetVariables(…);
SetGas();
SetMatrix();
SetSystem();

## Slide 7: Hands on the source code
Sciantix.C/h
Set
Update
Simulation
Simulation sciantix_simulation;
Burnup();
MapModel();
sciantix_simulation.Burnup();
…
InterGranularBubbleEvolution();
MapModel();
sciantix_simulation.InterGranularBubbleBehaviour();

## Slide 8: Hands on the source code
Sciantix.C/h
Set
Update
Simulation
FiguresOfMerit();
UpdateVariables(…);
Output();
output.txt

## Slide 9: Hands on the source code
Set
SetVariables.C/h
input_variable.emplace_back();
input_variable[iv_counter].setName("iFGDiffusionCoefficient");
input_variable[iv_counter].setValue(Sciantix_options[1]);
++iv_counter;
…
history_variable.emplace_back();
history_variable[hv_counter].setName("Temperature");
history_variable[hv_counter].setUOM("(K)");
history_variable[hv_counter].setInitialValue(Sciantix_history[0] * Sciantix_scaling_factors[4]);
history_variable[hv_counter].setFinalValue(Sciantix_history[1] * Sciantix_scaling_factors[4]);
history_variable[hv_counter].setOutput(1);
++hv_counter;
…
sciantix_variable.emplace_back();
sciantix_variable[sv_counter].setName("Xe produced");
sciantix_variable[sv_counter].setUOM("(at/m3)");
sciantix_variable[sv_counter].setInitialValue(Sciantix_variables[1]);
sciantix_variable[sv_counter].setFinalValue(Sciantix_variables[1]);
sciantix_variable[sv_counter].setOutput(1);
++sv_counter;
SetGas.C/h
void SetGas()
{
Xenon();
MapGas();
Krypton();
MapGas();
Helium();
MapGas();
}
SetMatrix.C/h
void SetMatrix( )
{
switch (int(input_variable[iv["iFuelMatrix"]].getValue()))
{
case 0:
{
UO2();
MapMatrix();
break;
}
…
SetSystem.C/h
void SetSystem()
{
switch (int(input_variable[iv["iFuelMatrix"]].getValue()))
{
case 0:
{
Xe_in_UO2();
MapSystem();
Kr_in_UO2();
MapSystem();
He_in_UO2();
MapSystem();
…

## Slide 10: Hands on the source code
Simulation
Simulation sciantix_simulation;
Burnup();
MapModel();
sciantix_simulation.Burnup();
…
InterGranularBubbleEvolution();
MapModel();
sciantix_simulation.InterGranularBubbleBehaviour();
Burnup.C/h
void Burnup()
{
model.emplace_back();
int modelIndex = model.size() - 1;
model[modelIndex].setName("Burnup");
…
Simulation.h
…
void Burnup()
{
/**
* Burnup uses the solver Integrator to compute the fuel burnup from the local power density. This method is called in Sciantix.C, after the definition of the Burnup model.
*/
sciantix_variable[sv["Burnup"]].setFinalValue(
solver.Integrator(
sciantix_variable[sv["Burnup"]].getInitialValue(),
model[sm["Burnup"]].getParameter().at(0),
physics_variable[pv["Time step"]].getFinalValue()
)
);
…

## Slide 11: Hands on the source code
Update
UpdateVariables.C/h
Sciantix_variables[0] = sciantix_variable[sv["Grain radius"]].getFinalValue();
Sciantix_variables[1] = sciantix_variable[sv["Xe produced"]].getFinalValue();
…

## Slide 12: Hands on the source code, objects
Fission gas / Helium
in UO2 / MOX
Fission gas / Helium behaviour
Production
Diffusion
(Solubility)
Interaction FG - He  bubbles

## Slide 13: Hands on the source code, objects
/// Derived class for gases (e.g., xenon, krypton, helium).
class Gas : virtual public Material
{
protected:
int atomic_number;
double mass_number;
double van_der_waals_volume;
double decay_rate;
double precursor_factor;
public:
void setAtomicNumber(int y)
{
/// Member function to set the atomic number of the fission gas
atomic_number = y;
}
…

## Slide 14: Hands on the source code, objects
/// Derived class for SCIANTIX models.
class Model : public HistoryVariable, public SciantixVariable, public InputVariable, public System
{
protected:
std::string overview;
std::vector<double> parameter;
public:
void setParameter(std::vector<double> p)
{
parameter = p;
}
std::vector<double> getParameter()
{
return parameter;
}
// Constructor & destructor
Model() {}
~Model() {}
};

## Slide 15
SCIANTIX: Advanced developments
Hands on the source code
Developer side: Editing and (re)compiling
Advanced modelling: Machine Learning with SCIANTIX
Survey
Giovanni Zullo
Lyon, France, 15.05.2024

## Slide 16: Developer side, Editing and (re)compiling
Intragranular gas diffusion
Fundamental parameters: diffusivity (single atoms), bubble nucleation, trapping, re-solution (w/ He solubility)
Physically-based single-size model derived from cluster dynamics (clusters with size n > 2 are counted as bubbles)
 intragranular gaseous swelling

## Slide 17: Developer side, Editing and (re)compiling
Intragranular gas diffusion
Fundamental parameters: diffusivity (single atoms), bubble nucleation, trapping, re-solution (w/ He solubility)
Physically-based single-size model derived from cluster dynamics (clusters with size n > 2 are counted as bubbles)
Source code? Adding a new diffusivity formulation for Xe/Kr in UO2
Default option:
From J.A. Turnbull, et al. IWGWRPT, IAEA, Preston (1988) 174-181.
Analytical expression based on CD atomic-scale calculations:
(from atomic to meso-scale)
From Matthews, C., et al. (2020). JNM, 540, 152326.
diffusivity (single atoms)

## Slide 18: Developer side, Editing and (re)compiling
How to compile a modified source code?
  Command line: issuing make command
  Command line: issuing cmake command / also cmake in visual studio
  Third-part programs (devc++, codeblocks, xcode, …)
Good practice:
  Did you modify the code? Always RUN the regression tests!

## Slide 19: Developer side, Editing and (re)compiling
Default option:
From J.A. Turnbull, et al. IWGWRPT, IAEA, Preston (1988) 174-181.
Analytical expression based on CD atomic-scale calculations:
(from atomic to meso-scale)
From Matthews, C., et al. (2020). JNM, 540, 152326.

## Slide 20: Developer side, Editing and (re)compiling

## Slide 21
SCIANTIX: Advanced developments
Hands on the source code
Developer side: Editing and (re)compiling
Advanced modelling: Machine Learning with SCIANTIX
Survey
Giovanni Zullo
Lyon, France, 15.05.2024

## Slide 22
FUEL SOLID FISSION PRODUCTS SWELLING
FUEL DENSIFICATION
GRAIN BOUNDARY VACANCY DIFFUSION
ATHERMAL FISSION GAS BEHAVIOUR
=
Advanced modelling, Machine Learning with SCIANTIX

## Slide 23
Corrective factor, λath
  Grain-edge inclination angle, θ
As-fabricated porosity, Pfab
Grain-edge length, l
Burnup, β
Temperature, T
Gas generation rate, S
Gas initial concentration, C0
single layer w/ 10 neurons
input layer
output layer
HF solver
Advanced modelling, Machine Learning with SCIANTIX

## Slide 24: Validity range of the FNN features
Quantity | Definition | Range |  | 
θ | Grain-edge inclination angle | 90 – 135 |  | °
Pfab | As-fabricated porosity | 2 – 9 |  | %
l | Grain-edge length | 3.67 – 11 |  | μm
β | Burnup | 0 – 50 |  | MWd kg-1
T | Temperature | 300-1600 |  | K
S | Gas generation rate | Irradiation | Annealing | at m-3 s-1
 |  | 1018 – 1020 | 0 | 
C0 | Initial concentration | Irradiation | Annealing | at m-3
 |  | 0 | 1019 – 1024 | 
Advanced modelling, Machine Learning with SCIANTIX

## Slide 25
Advanced modelling, Machine Learning with SCIANTIX
Chart: Burnup (MWd kgUO2-1)

## Slide 26
In conclusion
SCIANTIX: Advanced developments
Hands on the source code
Developer side: Editing and (re)compiling
Advanced modelling: Machine Learning with SCIANTIX
  Reference material: https://hdl.handle.net/10589/218541
Code repository: https://github.com/sciantix/sciantix-official
Contact
Giovanni Zullo: giovanni.zullo@polimi.it
Thanks for the attention!
Looking forward to your feedback